CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH881

Production date: Feb. 11, 2020~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH881 | Chameleonic | 36μm | ✘ | 120~150℃ | 3.5 | Hexagon | 0.08~3mm | ✔ | - | - | 7.0~7.5 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polybutylene Terephthalate* | *26062-94-2* | *607-857-5* | *93.8* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *2.8* |
| *Carbon Black (C.I. 77266)* | *1333-86-4* | *215-609-9* | *3.4* |

SECTION 4. TEST REPORT ON HEAVY METALS

