CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Holographic Blue Glitter Product code: FCHL700

Production date: Feb. 04, 2020~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness | Solvent-resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&CColorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCHL700 | Holographic Blue | 25μm |  | 160~170℃ | 4 | Hexagon | 0.08mm-3.0mm |  | - | - | 7.8 |  |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *97.66* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *1.8* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Yellow 5（CI.19140）* | *1934-21-0* | *217-699-5* | *0.03* |
| *FD&C Blue 1 (CI.42090)* | *3844-45-9* | *223-339-8* | *0.5* |

SECTION 4. TEST REPORT ON HEAVY METALS

