CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter Product code: FCHL401

Production date: Feb. 11, 2020~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat  Resistance | Light/UV  Resistance | Shape | size | FD&C  Colorant | D&C  Colorant | Pigment | PH Value | Surface  Degradability |
| FCHL401 | Holographic  Orange | 25μ/50μ | ✔ | 170~190℃ | 7 | Hexagon/Special  Shapes | 0.08~3mm | - | - | ✔ | 7.5~8 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *96.72* |
| *Acrylates copolymer* | *25133-97-5* | *618-355-0* | *2.2* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *Pigment Red 254 (CI.56110)* | *84632-65-5* | *401-540-3* | *0.46* |
| *Pigment Yellow 150* | *68511-62-6* | *270-944-8* | *0.61* |

SECTION 4. TEST REPORT ON HEAVY METALS

