CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Holographic Silver Glitter

Product code: FCHL100 batch number:20200220-A01 Production date: 20200219

Expiry date: 20230218

Supplier: Zhongshan Zhongtai pigments Co.,Ltd

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product Code | Color | Thickness | Solvent  -  resista nce | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCHL100 | Holographic  Silver | 25/50μm |  | 170~190℃ | 8.0 | Hexagon/Special  Shape | 3mm | - | - | - | 7.0-7.5 |  |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *98.89* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *1.1* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |

SECTION 4. TEST REPORT ON HEAVY METALS

