CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH11 Batch number: 20201108-A03 Production date: Nov. 1, 2020 ~ Dec. 24, 2020

Expiry date: Dec. 23, 2025

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

）

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness（μm | Solvent-resistance | HeatResistance | LightFastness | Shape | Size（mm） | FD&CColorant | D&CColorant | Pigment | PH Value | SurfaceDegradability |
| FCH11 | Iridescent Blue | 25/50 | no | 120~140℃ | 6-7 | Hexagon | 0.2 | ✔ | ✔ | / | 6.0~7.5 | no |

**SECTION 3. INFORMATION ON INGREDIENTS**

|  |  |  |  |
| --- | --- | --- | --- |
| ***Key Ingredient*** | ***CAS NO.*** | ***EC NO.*** | ***Target%*** |
| ***Polybutylene Terephthalate*** | ***26062-94-2*** | ***607-857-5*** | ***98.32*** |
| ***Acrylates Copolymer*** | ***25035-69-2*** | ***607-492-1*** | ***1.3*** |
| ***D&C Red 27 (CI.45410:2)*** | ***15876-58-1*** | ***240-012-5*** | ***0.01*** |
| ***FD&C Blue 1(CI.42090)*** | ***3844-45-9*** | ***223-339-8*** | ***0.37*** |

**SECTION 4. TEST REPORT ON HEAVY METALS**

## The test results are as follows:

**Remarks :** (1). 1 mg/kg = 0.0001% (2). MDL = Method Detection Limit （3). ND = Not Detected ( < MDL )

## German Health Authority BgA (Recommendation from German Health Journal No.28, July 1985)- Heavy Metals

Test Method : SGS in house method(SHTC® CHEM® SOP ®169®T), analysis was performed by ICP®MS.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test Item(s) | Unit | MDL | Test Result(s) | Limit |
| Lead (Pb) | mg/kg | 0.2 | ND | 20 |
| Cadmium (Cd) | mg/kg | 0.2 | ND | 5 |
| Arsenic (As) | mg/kg | 0.2 | ND | 5 |
| mercury(Hg) | mg/kg | 0.2 | ND | 1 |
| Antimony (Sb) | mg/kg | 0.2 | ND | 10 |

## German Health Journal No. 7/1992, Session 45 from November 14, 1991®Soluble Nickel

Test Method : Sample was extracted in 0.07mol/L HCI at 37℃,analysis was performed by ICP®OES.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test Item(s) | Unit | MDL | Test Result(s) | Limit |
| Soluble Nickel (Ni) | mg/kg | 5 | ND | 10 |

## To determine Lead content in the submitted sample in accordance with the CA Prop. 65.

Test Method : With reference to Inhouse method, analysis was performed by ICP-MS/ICP-OES.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test item(s) | Unit(s) | MDL | Test result(s) | Requirement(s) |
| \*Lead | mg/kg | 0.2 | ND | < 10 |

**\*** With refer to California proposition 65 announced on April 22, 2009 (Case no. H217587 (Consolidate with No. 01- 032306)), lead content will have to contain less than 5mg/kg for lipsticks and lipliners, while 10 mg/kg for eyeshadows and blushes.

## To determine Mercury content in the submitted sample in accordance with the US FDA 21 CFR 700.13.

Test Method : With reference to Inhouse method, analysis was performed by ICP-MS/ICP-OES.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test item(s) | Unit(s) | MDL | Test result(s) | Requirement(s) |
| Mercury | mg/kg | 0.2 | ND | < 1 |

## Chromium

Test Method : With reference to Inhouse method, analysis was performed by ICP-MS/ICP-OES.

|  |  |  |  |
| --- | --- | --- | --- |
| Test Item(s) | Unit | MDL | Test Result(s) |
| Chromium (Cr) | mg/kg | 0.2 | ND |