CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Iridescent Red Glitter Product code: FCH08 Batch number:20200408-B02 Production date: Apr. 01, 2020 ~ Apr.19, 2020

Expiry date:Apr.19, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness | Solvent-resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&CColorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH08 | Iridescent Red | 36μm |  | 120~150℃ | 3.5 | Hexagon | 0.08mm-3.0mm |  | - | - | 7.0-7.5 |  |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polybutylene Terephthalate* | *26062-94-2* | *607-857-5* | *97.98* |
| *Acrylates Copolymer* | *25133-97-5* | *607-559-5* | *1.60* |
| *FD&C Red 40 (CI.16035)* | *25956-17-6* | *247-368-0* | *0.42* |

SECTION 4. TEST REPORT ON HEAVY METALS

