CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Iridescent Glitter Product code: FCH03

Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH03 | Iridescent | 36μm |  | 120~150℃ | 8 | Hexagon/Special Shapes | 0.08mm-3.0mm | - | - | - | 7.8 |  |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polybutylene Terephthalate* | *26062-94-2* | *607-857-5* | *99.3* |
| *Acrylates Copolymer* | *25133-97-5* | *607-559-5* | *0.7* |

SECTION 4. TEST REPORT ON HEAVY METALS

