CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH913 batch number:20200406-A06 Production date: Apr. 11, 2020 ~ Apr.18, 2020

Expiry date: Apr. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH913 | Peony Red | 25/50μm | ✔ | 170~190℃ | 5 | Hexagon  /Special Shapes | 0.08~3mm | - | - | ✔ | 7.5~8 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *96.74* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *2.2* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Red 40 (CI.16035)* | *25956-17-6* | *247-368-0* | *0.66* |
| *D & C Red 27(C.I.45410:2)* | *15876-58-1* | *240-012-5* | *0.39* |

SECTION 4. TEST REPORT ON HEAVY METALS

