CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter Product code: FCH714

Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness | Solvent-resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&CColorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH714 | Light Blue | 25/50μm | ✘ | 160~170℃ | 3.5 | Hexagon/ Special Shapes | 0.08~3mm | ✔ | - | - | 7.5 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *97.57* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *1.8* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Blue 1 (CI.42090)* | *3844-45-9* | *223-339-8* | *0.62* |

SECTION 4. TEST REPORT ON HEAVY METALS

