CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Grass Green Glitter Product code: FCH620

Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH620 | Dark Green | 25/50μ m |  | 170~190℃ | 7.5 | Hexagon/Special shapes | 0.08mm-3.0mm | - | - |  | 7.5-8 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *96.23* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *2.2* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Blue 1（C.I. 42090）* | *3844-45-9* | *223-339-8* | *0.83* |
| *FD&C Yellow 5 （CI.19140）* | *1934-21-0* | *217-699-5* | *0.41* |
| *FD&C Red 40 (C.I.16035)* | *25956-17-6* | *247-368-0* | *0.32* |

SECTION 4. TEST REPORT ON HEAVY METALS

