CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH612

Production date: May 08, 2020 ~ May 22, 2020

Expiry date: May 22, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light Fastness | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH612 | Green | 25μm | ✘ | 160~170℃ | 3 | Hexagon | 1/128 inch | ✔ | - | - | 7~7.5 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| ***Key Ingredient*** | ***CAS NO.*** | ***EC NO.*** | ***Target%*** |
| ***Polyethylene terephthalate*** | ***25038-59-9*** | ***607-507-1*** | ***96.59*** |
| ***Acrylates copolymer*** | ***25133-97-5*** | ***607-559-5*** | ***2.6*** |
| ***Aluminum*** | ***7429-90-5*** | ***231-072-3*** | ***0.01*** |
| ***FD&C Blue NO. 1 (C.I. 42090)*** | ***3844-45-9*** | ***223-339-8*** | ***0.39*** |
| ***FD&C Yellow 5 （C.I.19140）*** | ***1934-21-0*** | ***217-699-5*** | ***0.41*** |

SECTION 4. TEST REPORT ON HEAVY METALS

