CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH406A batch number:20190216-A03 Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness | Solvent-resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&CColorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH406A | Light Brown | 25μm | ✔ | 170~190℃ | 6.5 | Hexagon | 0.08~3mm | - | - | ✔ | 7~7.5 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *95.71* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *2.6* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Red 40 (C.I.16035)* | *25956-17-6* | *247-368-0* | *0.66* |
| *FD&C Yellow 5 (C.I.19140)* | *1934-21-0* | *217-699-5* | *0.64* |
| *Carbon Black (C.I. 77266)* | *1333-86-4* | *215-609-9* | *0.38* |

SECTION 4. TEST REPORT ON HEAVY METALS

