CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH206 batch number:20200220-A02 Production date: Feb. 11, 2020 ~ Feb.28, 2020

Expiry date: Feb. 28, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Product  Code | Color | Thickness | Solvent-  resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C  Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH206 | Light Golden | 25μm/50μm | ✘ | 160~170℃ | 3 | Hexagon/Special  Shapes | 0.08~3mm | ✔ | - | - | 7~7.5 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *97.85* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *1.8* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |
| *FD&C Red 40 (C.I.16035)* | *25956-17-6* | *247-368-0* | *0.12* |
| *FD&C Yellow 5 （C.I.19140）* | *1934-21-0* | *217-699-5* | *0.22* |

SECTION 4. TEST REPORT ON HEAVY METALS

