CERTIFICATE OF ANALYSIS

# SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Silver Glitter

Product code: FCH001 batch number:20200221-A03 Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Dec. 11, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

# SECTION 2. INFORMATION ON SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ProductCode | Color | Thickness | Solvent-resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&CColorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| FCH001 | Silver | 25/50μ m |  | 170~190℃ | 8 | Hexagon/SpecialShapes | 0.08mm-3mm | - | - | - | 7.8 | Coating Layer Degradable |

SECTION 3. INFORMATION ON INGREDIENTS

|  |  |  |  |
| --- | --- | --- | --- |
| *Key Ingredient* | *CAS NO.* | *EC NO.* | *Target%* |
| *Polyethylene terephthalate* | *25038-59-9* | *607-507-1* | *99.17* |
| *Acrylates copolymer* | *25133-97-5* | *607-559-5* | *0.82* |
| *Aluminum* | *7429-90-5* | *231-072-3* | *0.01* |

SECTION 4. TEST REPORT ON HEAVY METALS

