Technical Data Sheet

| Product Name:1654 INCI Name: Synthetic Fluorphlogopite, Titanium Dioxide ，Silicon Dioxide and Tin Dioxide |
| --- |
| Composition | Specifications | Test Method |
| Synthetic Fluorphlogopite | 47-56% | ZTTM0307 |
| Titanium Dioxide | 10-14% | ZTTM0307 |
| Silicon Dioxide | 34-38% | ZTTM0307 |
| Tin Dioxide | 0-1% | ZTTM0307 |
| Appearance | Free flowing white powder | Visual |
| Particle Size | 20-100μm | ZTTM0301 |
| PH Value | 6-10 | ZTTM0304 |
| Odor | None | Organoleptic |
| Moisture | <1.0% | ZTTM0303 |
| Density | 2.9-3.5 g/cm3 | ZTTM0306 |
| Oil Absorption | 50-90 g/100g | ZTTM0305 |
| Heavy Metal |  |  |
| Composition | Specifications | Batch Value | Composition | Specifications | Batch Value | Test Method |
| Pb | ＜10 | Conform | Cd | ＜5 | Conform | ZTTM0308 |
| Hg | ＜1 | Conform | Ni | ＜10 | Conform | ZTTM0308 |
| Sb | ＜10 | Conform | Cr | ＜100 | Conform | ZTTM0308 |
| As | ＜2 | Conform | Cu | ＜50 | Conform | ZTTM0308 |
| Zn | ＜50 | Conform | Ba | ＜50 | Conform | ZTTM0308 |