

***SPECIFICATION***

**Coloron Pigment**

**(Code:SW060AY)**

|  |  |  |
| --- | --- | --- |
| ***Assay*** | ***Spec. Values*** | ***Test Method*** |
| ***Synthetic Fluorphlogopite*** | ***85.0-97.0%***  | ***CRTM-51*** |
| ***TiO******2***  | ***3.0-14.0%*** | ***CRTM-48*** |
| ***SnO2*** |  ***≤1.0%*** | ***CRTM-48*** |
| ***Particle Size*** | ***45-500 µm*** | ***CRTM-42*** |
| ***PH Value*** | ***6.0-10.0*** | ***CRTM-45*** |
| ***Density:*** | ***2.3-3.2g/cm3*** | ***CRTM-47*** |
| ***Oil absorption*** | ***60-150g/100g*** | ***CRTM-46*** |

**Zhongshan Zhongtai Pigment Co.,Ltd**

**Website: [http://www.zsztyl.com](http://www.zsztyl.com/) E-mail: zhongtaiyanliao@163.com**