| Raystar Glitter Green RS8297 |
| --- |
| Assay | Spec. Values | Test Method |
| Calcium Aluminum Borosilicate | 76.0-86.0% | CRTM-51 |
| TiO2 | 14.0-24.0% | CRTM-48 |
| SnO2 | ≤0.6% | CRTM-48 |
| Particle Size | 50-300µm | CRTM-42 |
| PH Value | 4-11 | CRTM-45 |
| Density: | 2.2-3.2g/cm3 | CRTM-47 |
| Oil absorption | 50-110g/100g | CRTM-46 |
| Aluminum Silicate CAS No: 1344-09-8; TiO2:C.I.No:77891; |