

***SPECIFICATION***

**Coloron Pigment**

***(Code:RS8289）***

|  |  |  |
| --- | --- | --- |
| ***Assay*** | ***Spec. Values*** | ***Test Method*** |
| ***Calcium Aluminum Borosilicate*** |  ***66.0-76.0%***  | ***CRTM-51*** |
| ***TiO2***  | ***24.0-34.0%*** | ***CRTM-48*** |
| ***SnO2*** | ***≤1.0%*** | ***CRTM-48*** |
| ***Particle Size*** | ***10-125 µm*** | ***CRTM-42*** |
| ***PH Value*** | ***4.0-11.0*** | ***CRTM-45*** |
| ***Density:*** | ***2.7-3.5g/cm3*** | ***CRTM-47*** |
| ***Oil absorption*** | ***50-85g/100g*** | ***CRTM-46*** |

**Zhongshan Zhongtai Pigment Co.,Ltd**

**Website: [http://www.zsztyl.com](http://www.zsztyl.com/) E-mail: zhongtaiyanliao@163.com**