| COSRAY Pearsl: Royal Gold (Code:6305C ) |
| --- |
| Assay | Spec. Values | Test Method |
| Synthetic Mica | 24.0-55.0% | CLRTM-51 |
| TiO2 | 40.0-60.0% | CLRTM-48 |
| Fe2O3 | 5.0-15.0% | CLRTM-48 |
| SnO2 | ≤1.0% | CLRTM-48 |
| Particle Size | 10-60 µm | CLRTM-42 |
| PH Value | 4.0-11.0 | CLRTM-45 |
| Density: | 2.7-3.7g/cm3 | CLRTM-47 |
| Oil absorption | 40.0-80.0g/100g | CLRTM-46 |
| Heavy Metals: |  | CLRTM -55 |
| As <3ppm Pb <10ppm Hg <1ppm Sb <2ppm Cd <1ppm Zn <50ppm Cr <100ppm Ni <200ppm |