

***SPECIFICATION***

**Coloron Pigment**

***(Code:2512Y）***

|  |  |  |
| --- | --- | --- |
| ***Assay*** | ***Spec. Values*** | ***Test Method*** |
| ***Calcium Aluminum Borosilicate*** |  ***50.0-60.0%***  | ***CRTM-51*** |
| ***TiO******2***  | ***1.0-10.0%*** | ***CRTM-48*** |
| ***SnO2***  | ***≤2.0%*** | ***CRTM-48*** |
| ***SiO2*** | ***20.0-30.0%*** | ***CRTM-48*** |
| ***Fe2O3*** |  ***10.0-20.0%*** | ***CRTM-48*** |
| ***Particle Size*** | ***10-125 µm*** | ***CRTM-42*** |
| ***PH Value*** | ***4.0-11.0*** | ***CRTM-45*** |
| ***Density:*** | ***2.3-2.8g/cm3*** | ***CRTM-47*** |
| ***Oil absorption*** | ***30-70g/100g*** | ***CRTM-46*** |

**Zhongshan Zhongtai Pigment Co.,Ltd**

**Website: [http://www.zsztyl.com](http://www.zsztyl.com/) E-mail: zhongtaiyanliao@163.com**