| Technical Data Sheet Product Name:1631 INCI Name: Synthetic Fluorphlogopite, Titanium Dioxide，Silicon Dioxide and Tin Dioxide |
| --- |
| Composition | Specifications | Batch Value | Test Method |
| Synthetic Fluorphlogopite | 34.2-55% | 45.7% | ZTTM0307 |
| Titanium Dioxide | 18-28% | 22.1% | ZTTM0307 |
| Silicon Dioxide | 27-37% | 31.6% | ZTTM0307 |
| Tin Dioxide | ≤0.8% | 0.6% | ZTTM0307 |
| Appearance | white powder | Conform | Visual |
| Particle Size | 10-60μm | > 80% within the range 10-60 μm | ZTTM0301 |
| PH Value | 6-10 | 6.21 | ZTTM0304 |
| Odor | None | Conform | Organoleptic |
| Moisture | <1.0% | 0.40% | ZTTM0303 |
| Density | 2.2-3.2g/cm3 | 3.04 g/cm3 | ZTTM0306 |
| Oil Absorption | 50-110g/100g | 90.4 g/100g | ZTTM0305 |
| Heavy Metal |  |  |  |
| Composition | Specifications | Batch Value | Composition | Specifications | Batch Value | Test Method |
| Pb | ＜10 | Conform | Cd | ＜5 | Conform | ZTTM0308 |
| Hg | ＜1 | Conform | Ni | ＜10 | Conform | ZTTM0308 |
| Sb | ＜10 | Conform | Cr | ＜100 | Conform | ZTTM0308 |
| As | ＜2 | Conform | Cu | ＜50 | Conform | ZTTM0308 |
| Zn | ＜50 | Conform | Ba | ＜50 | Conform | ZTTM0308 |